Alex Beck

4/28/04

# Garnet Project

Andradite Garnet sample was provided for analysis from Colorado. Sample was approximately a cubic centimeter in size. Sample was an uneven and ugly brownish yellow. Sample was broken up into pieces, powder was used for XRD analysis, while a small chunk was placed in epoxy gel for SEM scanning.

JMU XRD file 1707: 40 kV, 30 milliamp, step scan; 10-80 degrees two theta, step size .02, dwell time 0.5 seconds, 0.25 degrees two theta divergence slit.

After scan was completed several BCC A value spacing were determined:

(2 2 0) a = 11.9885 Å

(4 0 0) a = 12.0197 Å

(4 2 0) a = 12.0454 Å

(3 3 2) a = 12.0344 Å

(4 2 2) a = 12.0218 Å

(5 1 0) a = 12.0282 Å

Average:   12.023 Å

SEM settings: 325 spot size, 15mm working distance, 25 kV acceleration voltage, 2.794 amp filament current

SEM analysis of 5 points on epoxy mounted SEM sample are as follows:

Calculated empirical formula: (Ca2.626(≈3) Mn0.004) (Fe1.5832(≈2) Al0.018) (Si2.593(≈3) O12)

When the data was run through geological analysis program, the following results were achieved:

Determined Formula weight: 488.15 Atomic mass units                          Database value: 508.18 amu

Determined unit cell volume: 1737.96 Å3                                                 Database value: 1753.61 Å3

Determined density: 3.751 g/cm3   Database value: 3.849g/cm3  Measured database value: 3.26g/cm3